# SECTION 05 70 00

# Pre-Finished Metal Sheets

Go to https://www.azahner.com/document-library/ to verify that this is the most current version of the specification.

Use in conjunction with the Flat Sheet datasheet https://www.azahner.com/document/surfaces-product-datasheet/ to ensure correct selection of product thickness and size.

Contact Zahner for assistance with specifications and detail coordination: https://www.azahner.com/contact/

Optional items requiring selection by the specifier are in [blue]. Once selections are made and other options and brackets deleted, bold font and colored text should be reverted to match the balance of the document.

# GENERAL

## SECTION INCLUDES

### Section Includes: Pre-finished [copper] [stainless steel] [carbon steel] [weathering steel] [zinc] metal sheets that incorporate decorative pre-patinated surfaces.

### Related Sections:

#### Division 1: Submittal Procedures

#### Division 1: Quality Control

#### Division 1: Closeout Submittals

#### Division 5: Metal Fabrications

## RELATED SECTIONS

### Division 1 – General Requirements

#### Submittal Procedures

#### Quality Control

#### Closeout Submittals

### Division 5 – Metal Fabrications

## REFERENCE STANDARDS - Work shall comply with published recommendations of the following unless otherwise stated below:

### ZAHNER “Architectural Metals – A Guide to Selection, Specification and Performance”; John Wiley & Sons 1995: ISBN 0-471-04506-3.

### ZAHNER “Architectural Metal surfaces”; John Wiley and Sons 2005: ISBN 0-47126335-4.

### SMACNA “Architectural Sheet Metal Manual”.

### LEED – Leadership in Energy and Environmental Design.

#### [copper] ASTM B370 - Standard Specification for Copper Sheet and Strip for Building Construction.

#### [zinc] ASTM B69: Standard Specification for Rolled Zinc.

#### [stainless steel] ASTM A240: Standard Specification for Chromium and Chromium-Nickel Stainless Steel Plate, Sheet, And Strip for Pressure Vessels And For General Applications.

#### [stainless steel] ASTM A480: Standard Specification for General Requirements for Flat Rolled Stainless and Heat-Resisting Steel Plate, Sheet, and Strip.

#### [carbon steel] ASTM A1008/A1008M: Specification for Steel, Sheet, Cold-Rolled, Carbon, Structural, High-Strength Low-Alloy, High-Strength Low-Alloy with Improved Formability, Solution Hardened, and Bake Hardenable.

#### [aluminum] ASTM B209: Standard Specification for Aluminum and Aluminum-Alloy Sheet and Plate.

#### [aluminum] ASTM D2244: Standard Practice for Calculation of Color Tolerances and Color Differences from Instrumentally Measured Color Coordinates.

#### [aluminum] ASTM D4214: Standard Test Methods for Evaluating the Degree of Chalking of Exterior Paint Films.

### AAMA – American Architectural Manufacturers Association (www.aamanet.org).

#### [aluminum] AAMA 611: Voluntary Specification for Anodized Architectural Aluminum.

#### [aluminum] AAMA 2605: Voluntary Specification, Performance Requirements and Test Procedures for Superior Performing Organic Coatings on Aluminum Extrusions and Panels.

#### [aluminum] AAMA 609 & 610: Cleaning and Maintenance Guide for Architectural Finished Aluminum.

## SUBMITTALS

### Product Data: Submit manufacturer's Product Datasheet and installation instructions for custom Pre-Finished Metal Sheets, including material, finish, thickness, and dimensions.

### Samples:

#### Finish Selection Sample: If requested, provide up to 5 of each material finishes for Architect’s selection. Minimum Sample sizes: 8” x 10”

#### [Optional Mock-up Sheet]: If requested, provide a mock-up sheet to establish a quality standard for fabrication and installation. Subject to compliance with the requirement and approval, the mock-up sheet [may or may not] become part of the completed Work.

### Optional __% attic stock of purchased material is recommended (percentage to be filled out by specifier)

### Technical Datasheet: Submit technical data, including but not limited to pre-engineered structural calculation, system weight, and design pressure. [Project Specific engineering certification can be provided by the manufacturer at additional cost.]

### Closeout Submittals:

#### Warranty: Warranty documents specified herein.

#### Operation and Maintenance Instructions: Submit manufacturer's recommended cleaning and care instructions to properly maintain and prolong the service life of the metal panels.

### Sustainable Design Submittals:

#### [Angel Hair Stainless Steel] [GB-60 Stainless Steel] [Solanum Steel] [Oscura Blackened Steel] [Spectura Steel] Submit Product Specific (Type III) Environmental Product Declaration (EPD).

#### [Angel Hair Stainless Steel] [GB-60 Stainless Steel] [Solanum Steel] Submit IFLI Declare label.

#### Submit documentation from manufacturer for amount of pre-consumer and post-consumer recycled content for products specified.

#### Submit documentation providing location of manufacturing.

## QUALITY ASSURANCE

### Field Measurements: Contractor is responsible for providing final overall dimensions of the work surface area(s) prior to shop drawing submittal. At the Contractor discretion, this may be field verified dimensions. Information must be supplied in a format acceptable to the manufacturer.

### Manufacturer Qualifications:

#### Company specializing in manufacturing the quality products specified in this section with at least 15 years of documented experience and sufficient capacity to produce the required units within the Project Schedule.

#### Manufacturing location classified as a ‘zero-discharge’ waste water facility, or equivalent.

### Installer Qualifications:

#### Company specializing in installing the work of this section with at least 5 years of documented experience with comparable size project.

#### Familiar with the Products and the manufacturer’s installation methods.

### Source Limitation:

#### When possible, ensure all raw material came from the same producing mill, the same master slab, and the same chemical composition.

#### All sheets in this section shall be produced by the same manufacturer to protect against variations.

## DELIVERY, STORAGE, AND HANDLING

### Delivery and Receipt:

#### Deliver products in factory sealed and labeled packages.

#### All crates and packaging should be inspected upon delivery for damage. Contact the manufacturer immediately at the time of receipt if any damage is identified. Photographs of any damaged product, including concealed damages, must be supplied to the manufacturer with any claims. Photos of damaged crates and packaging must also be provided to manufacturer.  Freight damage must be filed with freight company within the freight carrier’s terms.

### Storage and Transportation:

#### Keep packaging units dry while in secure and locked storage and transport.

#### Keep panels dry prior to installation.

#### Crated products that are stored under tarps should be frequently opened and ventilated to reduce humidity and condensation accumulation.

#### Do not lay any protective mats or covers directly on top of panels.

#### Do not store panels in contact with other materials that might cause staining, denting, or other surface damage.

#### Crates and packaging: Do not stack crates unless otherwise approved and noted by manufacturer.

#### Do not lay any exposed and finished face against another surface or another panel for any length of time. Water will accumulate between the surfaces and cause an accelerated oxidation on the patina.

### Handling and Installation:

#### Keep film-protected products dry and out of direct sunlight until installation.

#### Remove the protective film immediately after installation.

#### Require all personnel to wear clean white cotton gloves when handling and installing architectural metal panels.

#### Keep product free of oil, grease, mortar, paint, acid, bitumen, drilling dust, dirty water, and other impurities.

#### Do not use adhesive tape on products in areas visible after installation.

#### Do not scribe or mark on products.

### Protection:  The Contractor is responsible to use all means necessary to protect the materials of this Section before, during and after installation and to protect the installed work and materials of all other trades.

### Site Conditions: Adjoining substrate and structure for attachment to be complete. Installation subject to state of increment weather.

### Replacements: In the event of damage, immediately make all repairs and replacements necessary at the sole cost of the responsible party.

## WARRANTY

### Manufacturer’s Warranty: Manufacturer will warrant its products to be in good quality, free from defects, in conformance with the specification, and when installed in accordance with manufacturer’s published installation procedures. Any defaults or defects in material or workmanship resulting solely from the manufacturer shall constitute a warranty claim. Manufacturer’s warranty coverage and failure types includes, but not limited to, the following:

#### 1-year limited warranty on deterioration of metals, defined as perforation due to corrosion resulting from manufacturer’s defects, and loss of adhesion as a result from manufacturer’s finish application. Damage to or failure of the product caused by the improper handling or cleaning will not be covered. This warranty does not cover natural weathering and fading of the surface that will occur as the surface is exposed to ambient conditions. Nor does it cover minor oxidation or oxidation products that transfer to other surfaces.

#### Warranty commences upon shipment of material by manufacturer.

#### During the warranty period, and upon approval of the claim, the manufacturer will repair, or at its option, replace the products that are proven to be defective. The labor and all associated costs (i.e., Scaffolding, lifts, etc.) to remove and reinstall repaired or replacement product is not included.

# PRODUCT

## MANUFACTURERS

### Basis of Design: A. Zahner Company

#### Product Website: https://www.azahner.com/products/sheets/

#### Address: 1400 E. 9th Street, Kansas City, MO 64106

#### Phone: +1 (816) 423-8354

### Request for substitutions will be considered in accordance with provisions in [Section 01 60 00]

## PERFORMANCE CRITERIA

### Patina Performance

#### Surface to be comprised of a patina constituted of an oxide layer that, in both chemistry and structure, replicates a naturally occurring, mature patina. Variations in the appearance of the patina, within individual sheets or between multiple sheets, are normal and expected. Metal patinas will continuously develop and evolve over time in response to ongoing reactions to atmospheric influences. The natural evolution or variation in appearance because of these reactions is a feature of the metal and does not constitute a defect.

## MATERIALS

### Solanum Steel [1-sided] [2-sided]

#### Material: Weathering Steel A588/A606-4.

#### Sheet Width: 48” (maximum 60” depending on thickness)

#### Sheet Length: 120” (maximum 144” depending on thickness)

#### Sheet Thickness: [0.048” 0.060” 0.075” 0.105” 0.120” 3/16”]

### [Oscura Blackened Steel] [Spectura Steel]

#### Material: Carbon Steel 1008A

#### Sheet Width: 48” (maximum 60” depending on thickness)

#### Sheet Length: 120” (maximum 144” depending on thickness)

#### Sheet Thickness: [0.036” 0.048” 0.060” 0 .075” 0.105” 0.120”]

### [Dirty Penny Copper] [Star Blue Copper]

#### Material: Copper

#### Sheet Width: 36”

#### Sheet Length: 120”

#### Sheet Thickness: [20 oz (0.0270”)  24 oz (0.0323”)  32 oz (0.0431”)  48 oz (0.0646”)]

### [Angel Hair Stainless Steel] [GB-60 Stainless Steel] [1-sided] [2-sided]

#### Material: Stainless Steel [Type 304]  [Type 316L]

#### Sheet Width: 48” (maximum 60” depending on thickness)

#### Sheet Length: 120” (maximum 144” depending on thickness)

#### Sheet Thickness: [0.038” 0.050” 0.063” 0 .078” 0.109” 0.125”]

### [Fuscara Blackened Stainless Steel]

#### Material: Stainless Steel [Type 304]

#### Sheet Width: 48”

#### Sheet Length: 120”

#### Sheet Thickness: [0.038” 0.050” 0.063” 0 .078” 0.109” 0.125”]

### [Baroque Zinc] [Hunter Zinc] [Roano Zinc]

#### Material: Zinc

#### Sheet Width: 39.4”

#### Sheet Length: 120”

#### Sheet Thickness: 0.032” (0.8mm)

## FIRE PERFOMANCE

### [Solanum Steel] [Oscura Blackened Steel] [Spectura Steel] [Roano Zinc] When tested in accordance with ASTM E84, materials shall have a Flame Spread Index of 0 and a Smoke Developed Index of 0.

### [Star Blue Copper] When tested in accordance with ASTM E84, materials shall have a Flame Spread Index of 0 and a Smoke Developed Index of 5.

# EXECUTION

## SITE CONDITION VERIFICATION

### Verify substructure’s location and condition are suitable for installation of the pre-finished metal sheets in accordance with the manufacturer’s specification.

### Complete visual inspection of substructure surface to ensure a smooth and continuous surface that can withstand the required loads without deflection or deformation and that is capable of receiving the required fasteners (if required) for the system. Correct any conditions detrimental to the proper and timely completion of the work. Do not proceed with the work until unsatisfactory conditions are corrected to permit proper installation of the work.

## FABRICATION

### Fabricate pre-finished metal sheets in compliance with the drawing details which include design, dimensions, geometry, metal thickness and other characteristics.

### [Oscura Blackened Steel] Reapply factory clear coat following any fabrication.

### Allow sufficient room for expansion in the material to prevent buckling, damage, and deterioration of the Work.

## SITE PREPARATION

### Examine substrate and ensure surfaces are clean and clear of all obstacles and debris.

## INSTALLATION

### Comply with manufacturer's instructions for assembly, installation, and erection of pre-finished metal sheets.

## CLEANING AND PROTECTION

### Remove protective film from exposed surfaces of metal panels promptly upon installation and in accordance with manufacturer’s recommendations and with care to avoid damage to finish.

### Clean exposed surfaces of custom metal panel work promptly after completion of installation. Comply with the recommendations of the panel manufacturer.

### Maintain installed custom panels in a clean condition throughout construction and ensure that cleaning by other trades in proximity to the custom panels does not impart dust or debris on panels. Avoid spilling, dripping, or splattering cleaning solutions onto custom panels.

# End of Section